## Slide 1: Next Two Steps in Improving HMA
56th Annual Bituminous Conference
Matt Mueller
Engineer of Tests
Illinois Dept. of Transportation
Jim Trepanier
HMA Operations Engineer
Illinois Dept. of Transportation
Notes: Thank you _______ & Good Morning. Well the first thing you will probably notice is that I changed the title of this presentation. As ______ indicated this presentation will be co-presented. I will present the first step in improving HMA and Matt Mueller will present the second step.

## Slide 2: Next Steps in HMA Improvement
Tack Coat
Hamburg Wheel
QCP
PFP
FRAP
Super
Pave
Field
VMA
Notes: As you can see we have made some major strides in improving HMA over that last couple decades. Listed here are just a few and now we are ready to add two more that we believe will dramatically increase the life of our HMA pavements.
This is going to be very important at a time of shrinking budgets when there is a real need to make our pavements last longer.

## Slide 3: HMA Quiz
What is the leading HMA distress driving pavement rehabilitation?
  Loss of Friction
  Wheel Path Rutting
  Raveling
  Premature Cracking
  Raveling & Cracking at the Centerline Joint

## Slide 4: Deteriorated Joint

## Slide 15: Answer
What is the leading HMA distress driving pavement rehabilitation?
  Loss of Friction
  Wheel Path Rutting
  Raveling
  Premature Cracking
  Raveling & Cracking at the Centerline Joint

## Slide 16: Why the Poor Performance?

## Slide 17: Deteriorated Joint
How many years?

## Slide 18: How many years?

## Slide 19
Maintenance - Disruptive and Dangerous

## Slide 20: Next Step in HMA Improvement
Super
Pave
Tack Coat
Hamburg Wheel
QCP
PFP
FRAP
Long Joint Seal
Super
Pave

## Slide 21: Efforts to Minimize Permeability along Longitudinal Joints
2001/2002 Longitudinal Joint Sealants
  IDOT worked w/ 2 companies to Develop a Longitudinal Joint Sealant (LJS)
  LJS is a Band of Asphalt Binder that Seals a lift of HMA from the Bottom Up.
  Here is How it Works:

## Slide 22: Joint Sealant Concept
Band melts up into the joint thus:
  Increasing density
  Decreasing permeability
  Increasing joint life
Unconfined
18 inches
Joint Sealant

## Slide 23: Asphalt Materials/Hendy Quickseam

## Slide 24: Longitudinal Joint Seal

## Slide 25: Longitudinal Joint Seal 12 Yrs Later

## Slide 26: Longitudinal Joint Seal 12 Yrs Later
No LJS
LJS

## Slide 27
Shear Tears

## Slide 28: Effect of In-Place Voids on Life Washington State DOT Study
Chart: In-situ Air Voids, %
| 7 | 8 | 9 | 10 | 11
Remaining Service Life, Years | 100 | 98 | 94 | 83 | 64
93% 92% 91% 90% 89%
Compaction Level
Notes: This Washington study is often referenced. It highlights the relationship between in-place pavement air voids and pavement service life.
With longitudinal joint densities typically at 90% or less it is easy to explain those opening photos of premature joint failures. At ninety percent compaction (10-percent air voids) we can expect joint performance to be: joint performance = mat performance – 1/5.
When joint density drops to 89% then joint performance can expect to be: joint performance = mat performance – 1/3. For a 15 year expected mat performance, giving up 1/5th means the joints fail 3 yrs earlier than mat (giving up 1/3rd means the joints fail 5 yrs earlier).

## Slide 29: Heavy Duty Pressure Distributor for Applying LJS

## Slide 30: Heavy Duty Pressure Distributor for Applying LJS

## Slide 31: Five Minutes After Placement

## Slide 32: Paving over LJS

## Slide 34: Licensed Subcontractor ≈ 11 Trucks

## Slide 35: Cost Comparison
Inlay: $8.00 / lineal ft
  Includes: traffic control, mobilization, milling, priming, paving, pavement marking
Microsurfacing: $4.81 / lineal ft
  Includes: crack seal, traffic control, pavement marking/removal
Route and Seal: $2.00 / lineal ft
  Includes: prime, crack seal, traffic control
Longitudinal Joint Seal: $2.00 lineal ft

## Slide 36: Cost Comparison
Inlay: $8.00 / lineal ft
  Includes: traffic control, mobilization, milling, priming, paving, pavement marking

## Slide 37: Cost Comparison
Microsurfacing: $4.81 / lineal ft
  Includes: crack seal, traffic control, pavement marking/removal

## Slide 38: Cost Comparison
Route and Seal: $2.00 / lineal ft
  Includes: crack seal, traffic control

## Slide 39: Cost Comparison
Longitudinal Joint Seal: $2.00 lineal ft

## Slide 40: Also Works as a Tack Coat

## Slide 41: Longitudinal Joint Spec
Implementation Goals:
  2016 – 2 Projects per District
  2017 – 50% of Projects per District
  2018 – Full Implementation

## Slide 42: Next Step in HMA Improvement
Long. Joint Seal
Tack Coat
Hamburg Wheel
QCP
PFP
FRAP
Retire

## Slide 43: Next Step in HMA Improvement
Long. Joint Seal
Implement I-FIT
Tack Coat
Hamburg Wheel
QCP
PFP
FRAP

## Slide 44: Illinois Flexibility Index Test I-FIT
A Performance Test Just Like Hamburg Wheel
Uses a Semi-Circular Bend (SCB) Test Fixture with a Gyratory or Core Specimen
The Test Can Be Completed in a Day
Owners Can Use the Results for QA
Contractors Can Use the Results for Optimizing Profit and Trouble Shooting
Material Suppliers Can Use the Results for Marketing Products/Modifiers

## Slide 45: Illinois SCB set-up

## Slide 47
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Lab Mix

## Slide 48
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Severe Production Induced Damage
Cold Stockpiles

## Slide 49
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Severe Production Induced Damage
Cold Stockpiles
Silo Storage

## Slide 50
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Severe Production Induced Damage
Cold Stockpiles
Silo Storage
Wet Recycle

## Slide 51
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Severe Production Induced Damage

## Slide 52
Chart: FI -vs- Years
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Severe Production Induced Damage

## Slide 53
Possible Solution: Add a Modifier to Production Mix to Minimize Damage

## Slide 54
Chart: FI -vs- Years with Modifier
| 0 | 0 | 1 | 2 | 5 | 10 | 14
ALF Fatigue Cycles | 12 | 10 | 8 | 6 | 4 | 2 | 1
Lab Mix

## Slide 55: I-FIT Implementation
The Department
  is looking at the January and March 2016 lettings for Experimental Feature Projects
  has On-going Round-Robin Testing with Private Labs with SCBs
  is Testing any Contractor Plant Produced Mix Delivered for Testing
  has Two more SCBs on Order
Industry has Begun Testing
Academia is Researching More Applications of the I-FIT protocol

## Slide 56: Questions