## Slide 1: National Performance of High Recycled Mixtures

## Slide 2: Outline
Trends in RAP and RAS usage and practices
Motivations for higher recycled contents
Barriers to higher recycled contents
Research and future directions

## Slide 3: Estimates of RAP Usage
NAPA surveys estimate that the national average RAP content increased from 16.2% in 2009 to 20.4% in 2014.
  RAP contents tend to be higher in commercial projects compared to government projects.
RAP usage varies considerably from state to state.

## Slide 4: Average RAP contents by state
NAPA IS 138, 2015

## Slide 5: Motivations for Higher RAP Contents
Environmental & Sustainability benefits
Economic savings

## Slide 6: Conservation of Materials
At an average RAP content of 20%, we conserve over 66 million tons of aggregate and 9 million barrels of asphalt each year.

## Slide 7
The average RAP content in Japan is 47%

## Slide 8
Chart: Unmodified Paving Grade Asphalt and Crude Oil Prices
Notes: Over the last decade asphalt binder prices tripled and this put tremendous pressure to try to be more economical and cut costs in mix designs and mix production.

## Slide 9: Current RAP Practices
In most (not all) places across the USA…
Project millings become property of contractor
Urban contractors have excess supplies of RAP
Processing options for RAP
  no additional processing for single source milling stockpiles
  blending & crushing: multiple source stockpiles
  fractionating: RAP contents >30%

## Slide 10: Reasons why Contractors use less RAP than allowed
Availability of RAP
Requirement to use a softer virgin binder
  Limited availability and/or tankage issue
  Requirement to recover and Test RAP binder
Ability to control the quality of the mix
  Moisture
  Amount of material passing no. 200 sieve
  Workability
  RAP variability

## Slide 11: Barriers to Higher RAP Contents
History and Perceptions
  Performance of high RAP content pavements
  Concerns about quality and consistency of RAP
Technology Limitations
  Current mix design system
    Relies on VMA & therefore aggregate bulk specific gravities
    Does not adequately consider composite binder properties
  Need reliable performance tests

## Slide 12
LTPP SPS-5 pavement sections
18 U.S. states and Canadian provinces
Eight 500 ft. test sections
Rehabilitated sections compared
  2” vs 5”overlay thickness
  RAP (30%) vs virgin mixes
  Milled vs unmilled surface preparation
Projects range in age from 6 to 17 yrs
Performance Study of Asphalt Pavements with Greater than 25% RAP

## Slide 13: SPS-5 Project Locations

## Slide 14: ANOVA: Rutting

## Slide 15
ANOVA: Fatigue Cracking

## Slide 16
ANOVA: Transverse Cracking

## Slide 17: ANOVA: International Roughness Index

## Slide 18: Conclusions on LTPP SPS-5
Based on a long-term performance analysis of a large number of projects across North America…
Pavements using ≥ 30% RAP performed well, and in most cases, perform equal or better than virgin pavements
Transverse and fatigue cracking were observed at higher percentages in pavements with RAP compared to pavements with all virgin materials.
  Higher percentages cracking did not impact overlay lives
  Mix designs on several projects indicate high dust contents and low asphalt contents for RAP mixes.

## Slide 19: Barriers to Higher RAP Contents
History and Perceptions
  Performance of high RAP content pavements
  Concerns about quality and consistency of RAP
Technology Limitations
  Current mix design system
    Relies on VMA & therefore aggregate bulk specific gravities
    Does not adequately consider composite binder properties
  Need for reliable performance tests

## Slide 20: NCAT Research on Using Recycled Materials
NCHRP 9-46: high RAP content mix design
Lab studies on how to improve cracking resistance for mixes containing RAP and RAS
NCHRP 9-53: Combining RAS & WMA
Test Track experiments in 3rd, 4th, 5th, and 6th cycles
  High RAP contents
  RAS
  GTR

## Slide 21
Method 1: Recover aggregate using a solvent extraction, then conduct AASHTO T84 and T85 on the fine and course fractions like any other aggregate.
RAP Aggregate Bulk Specific Gravity
Method 2: Recover aggregate by the ignition method, then conduct AASHTO T84 and T85 on the fine and course fractions like any other aggregate.

## Slide 22: RAP Aggregate Bulk Specific Gravity
Method 3: Estimated Gsb from Gmm & Pba
  Determine Gmm (w/ dryback) of RAP sample
  Calculate Gse using Eq. 1:
  Estimate the absorbed asphalt, Pba , based on historical values for the plant location.
  Calculate Gsb using Eq. 2:
Equation 1
Equation 2

## Slide 23: Recommendations RAP Aggregate Gsb
One method of determining RAP aggregate Gsb will not work for all material types. Agencies should evaluate options to find the best method for their materials. The method that gives the lowest Gsb will result in the lowest mix VMA. This is desirable since it will lead to higher asphalt contents and better durability.

## Slide 24: Some Tests for Assessing Cracking Resistance
SCB-LA
Energy Ratio
OT-NCAT
Cantabro
I-FIT
OT-TX
Nflex Factor
BBF
DCT
SVECD
Notes: We need to find a cracking test that we can count on to indicate performance. Actually, it may be different tests for different forms of cracking. But this webinar is not going to get into the pros and cons of the different tests.

## Slide 25: NCAT Test Track
2006: Moderate and High RAP Content Surface Mixes
Mixes with 20% and 45% RAP performed very well
30 million ESALS over 8 years
Minor differences in cracking support the use of softer binder for high RAP content mixes
Lab Tests: Bending Beam Fatigue, Energy Ratio, Texas Overlay Tester
  Best correlation with top-down cracking in sections was IDT Creep Rate

## Slide 26: NCAT Test Track
2009: Virgin versus 50% High RAP Content – All Layers
Mixes with and without WMA
All sections performed very well
50% HMA section – no distress through 20 million ESALS
Lab Tests: BBF, Overlay Tester, SVECD
  Best correlation with observed fatigue cracking was OT results extrapolated to measured strain level

## Slide 27: Cold Central Plant Recycling
Sponsored by Virginia DOT
Processed RAP 2% foamed asphalt and 1% cement
Serves as base layer with overlays of 4 inches and 6 inches
Objective: quantify the structural contribution (empirical and M-E)
Performance has been outstanding – no distress 11 MESALs and counting

## Slide 28: NCAT Test Track
2015: Cracking Group Experiment: Top-Down Focus
7 surface mixes with a range of expected cracking resistance
Lab Tests: I-FIT, SCB-LTRC, Overlay Test, Energy Ratio, & others

## Slide 29: 2016 MnROAD Thermal Cracking Experiment
16
17
23
22
21
20
19
18
Transition zones

## Slide 30: Recycled Asphalt Shingles Usage
Hansen and Copeland, Annual Asphalt Pavement Industry Survey on Recycled Materials and Warm-Mix Asphalt Usage: 2009-2014
Chart: Percentage, %
| 2009 | 2010 | 2011 | 2012 | 2013 | 2014
DOTs | 0.33 | 0.78 | 0.66 | 0.83 | 0.85 | 0.72
Other Agencies | 0.37 | 0.47 | 0.93 | 0.9 | 1.08 | 0.95
Commercial & Residential | 0.63 | 0.81 | 1.04 | 1.24 | 1.24 | 1.47
Notes: Like RAP, RAS usage has been on the increase over the past 5 years. In 2013, there was a slight decrease in the national average; however, both DOT and other agency work increased. The decrease was seen in private work.

## Slide 31: Recycling Asphalt Shingles
Currently used in about 37 states, but routinely for state DOT projects in only about a dozen states
Typically 3 to 5% RAS by weight of mix
Field performance has been mixed
Mix design approaches continue to evolve

## Slide 32: Performance of Mixes with RAS
Virgin Mix
PG 76-22 SBS
Virgin Mix
PG 76-22 GTR
20% RAP Mix
PG 76-22 SBS
20% RAP + 5% RAS
PG 76-22 SBS

## Slide 33: Research and future directions
Validation of mix cracking tests
“Balanced” mix designs will replace volumetric-based mix designs
Rejuvenator formulations will mature
Much higher RAP content asphalt mixtures
Cold recycled 100% RAP (with some minor additives) as base layer for heavy traffic roads and as a primary structural layer in light traffic pavements.

## Slide 34: Thank You!